## Slide 1
paul-egan.com
Design and testing of 3D printed tissue
scaffolds with directionally tunable stiffness
Abdullah Al Masud
Paul Egan
Amit Arefin
Ming-Chien Chyu
Dept. Mechanical Engineering
Texas Tech University
Abdullah Masud
Paul Egan

## Slide 2: Medicine, Mechanics, and Manufacturing Design (M3D) Lab
Tissue Scaffolds
Personalized Nutrition
Integrated Design
for
Medical Innovations

## Slide 3: Background: Bone tissue scaffold printing
Tissue scaffold design
Mimic bone geometry
Potentially complex loading cases
Requires biocompatibility
Must achieve high porosity
Wieding et. al. Med. Eng. Phys. 2013
Blazquez-Carmona et. al. J. Mech. Behav. Biomed. Mat. 2021

## Slide 4: Aim: Design bone scaffolds with bi-axial tuning
Bi-axial tuning
Systems have asymmetric loads
Unit cells in lattices can have their geometry modified appropriately
Unit cells are patterned to form scaffolds of specified geometries

## Slide 5: Methods: Scaffold fabrication
Printing process
EnvisionTEC DLP printing
E-shell 600 Methacrylic acid-based resin
Build-direction may affect mechanics

## Slide 6: Methods: Mechanical testing orientation
Compression testing
Fixed ends interface with compression plates
Orientation of fixed ends and build direction dictate whether Ez or Ex elastic moduli tested

## Slide 7: Results: Porosity differences
Mechanical testing
Higher porosity leads to higher longitudinal elastic modulus
Higher unit cell length leads to higher longitudinal elastic modulus

## Slide 8: Results: Porosity differences
Mechanical testing
Higher porosity leads to higher longitudinal elastic modulus
Higher unit cell length leads to higher longitudinal elastic modulus

## Slide 9: Results: Stretching unit cell height
Trends
Higher unit cell height increases elastic modulus
Not perfectly linear, could have manufacturing affect mechanics

## Slide 10: Results: Biaxial loading
Mechanical results
Longitudinal elastic modulus Ez is greater than tranvserve elastic modulus Ex only for stretch designs.
Increase in Ez is sharper than decrease in Ex as designs are stretched

## Slide 11: Results: Fabricated scaffolds
Scaffold testing
Longitudinal stiffness of 10 kN/mm for bone tissue engineering
By stretching the design you increase stiffness in Ez while maintaining stiffness in Ex
Egan et. al. J. Mech. Des. 2019

## Slide 12: Discussion: Manufacturing affects mechanics
Limitations
Checking print defects and porosity influences
Can’t test every condition
Future work
Greater characterization of printing defects and failures
Design, build, and test for scaffold viability in use case

## Slide 13: Conclusion: Biaxial tuning is viable
Key takeaways
Scaffolds qualitatively printed in a number of varied configurations for porosity and unit cell design
Can tune mechanics in multiple directions with varying relative trade-offs
Viable for scaffold problem in terms of overall stiffness, further optimization and testing needed

## Slide 14
Thank you
paul-egan.com